| RDC-CONEX is a reduction clearing agent for Polyester and its blends. RDC-CONEX is very convenient to control the process, because it shows good reduction clearing effect even when used alone without Sodium Hydroxide or Sodium Hydro Sulfide. |  |
| --- | --- |
| ◈ SPECIFICATION - APPEARANCE - IONIC NATURE - pH (1% aq. Sol'n) - SP.GR(at 25℃) - SOLUBILITY - STORAGE STABILITY - COMPATABILITY ◈ FEATURES ◈ APPLICATION FIBERS ◈ HOW TO USE | White Powder Nonionic 10.5 ± 1.0 1.05 ± 0.05 Easily soluble in warm water (above 40℃). Min. 1 year under cool and dry conditions when stored in original sealed, packaging. Compatible with anionic, nonionic and cationic materials. - RDC-CONEX shows good reduction clearing effect when used on polyester and T/C fibers dyed with disperse dyestuff and it improves color, washing and rub fastnesses. - RDC-CONEX shows excellent efficiency on reducing and removing the stained disperse dyestuff on cellulose fiber after T/C fiber is dyed with disperse dyestuff, continuously keeping strong reductive power. - RDC-CONEX , low foaming, doesn't affect sublimation and light fastnesses. - It is environmental-friendly product as APEO-free and NPEO-free. Suitable for fibers such as Polyester, T/C, N/P, etc. Recommended use levels are 1-4 g/ℓ according to kinds of dyeing materials and the concentration of color. |

| ◈ RECOMMENDED RECIPE | 1) Polyester goods dyed in medium color |  |
| --- | --- | --- |
|  | - Amount Required of RDC-CONEX - Reduction clearing conditions - Washing conditions | : 1-2 g/ℓ : Treat for 20∼25 min at 75-85℃. : Washing hot and then cold. |
|  | 2) Polyester goods dyed in dark color |  |
|  | - Amount Required of RDC-CONEX - Reduction clearing conditions - Washing conditions | : 2-4 g/ℓ : Treat for 20∼25 min at 75-85℃ : Washing hot and then cold. |
| 3) Interim reduction clearing in 2 bathes dyeing of T/C fiber |  |  |
|  | - Amount Required of RDC-CONEX - Reduction clearing conditions - Washing conditions | : 4-8 g/ℓ : Treat for 20-25 min at 75-85℃ : Washing hot and then cold. |
| ◈ NOTICE ◈ PACKAGE | - Please avoid storing in place of high humidity. - Please use an excess quantity in the case of the interim reduction clearing for 2 bathes dyeing of T/C fiber. 100 Kgs NET IN DRUMS. |  |