| BARANOL-AC is a specific surfactant devised to remove oil spots which may be generated in a sizing process. |  |
| --- | --- |
| ◈ SPECIFICATION - APPEARANCE - IONIC NATURE - pH(1% aq. Sol'n) - SP.GR (at 25℃) - SOLUBILITY - STORAGE STABILITY - COMPATABILITY ◈ FEATURES ◈ APPLICATION FIBERS ◈ HOW TO USE | Light Yellowish Liquid Nonionic 7.0 ± 1.0 1.05 ± 0.05 Easily soluble in cold water. Min. 1 year under cool and dry conditions when stored in original sealed, packaging. Compatible with anionic, nonionic and cationic materials. - BARANOL-AC completely disperses and removes oil and various stains which are not easily removed in a general scouring process and whiteness is good because it shows excellent emulsifying/penetrating capability. - BARANOL-AC is no harm to fiber and does not cause troubles such as a yellowing and so on. - BARANOL-AC can be applied to all kinds of fibers. - Its efficiency can be more improved when BARANOL-AC is used with an alkali agent such as NaOH, because it has good chemical, acid and alkali resistances. - It is environmental-friendly product as APEO-free and NPEO-free. Suitable for all fibers such as Polyester, Nylon, Cotton, T/C, N/C, etc. Recommended use levels are 1-3 g/ℓ according to kinds, density, thickness and types of fibers. |

| ◈ RECOMMENDED RECIPE | 1) Scouring method of non-sized high density polyester and Nylon goods |  |  |
| --- | --- | --- | --- |
|  | - 98% NaOH - Na2CO3 - QX-801 - BARANOL-AC - Scouring conditions - Washing conditions - Bath ratio |  | : 4-5 g/ℓ : 1-2 g/ℓ : 2 g/ℓ : 2 g/ℓ : Scouring for 60min at 100℃. : Washing hot and then cold. : 1:10-1:30 |
| 2) Scouring method of sized high density polyester and Nylon goods |  |
|  | - 98% NaOH - ACMR-70 - QX-801 - BARANOL-AC - Scouring conditions - Washing conditions - Bath ratio |  | : 4-5 g/ℓ : 2 g/ℓ : 2 g/ℓ : 2 g/ℓ : Scouring for 60min at 100℃. : Washing hot and then cold. : 1:10-1:30 |
| ◈ PACKAGE | 120 Kgs NET IN DRUMS. |  |  |