After bleaching cellulose based fiber such as cotton and blended fabrics with the hydrogen peroxide, peroxides can remains in fiber due to washing insufficiency.

In this case if you do dyeing with the reactive or direct dyestuffs, troubles including concentration decline/change of color, dyeing spots, dyeing stains etc may arise.

AC-K  makes the above troubles prevent because it has good removal efficiency against remaining peroxides.

| ◈ SPECIFICATION - APPEARANCE - IONIC NATURE - pH(as is) - SP.GR(at 25℃) - SOLUBILITY - STORAGE STABILITY - COMPATABILITY ◈ FEATURES ◈ HOW TO USE ◈ RECOMMENDED RECIPE | Uniformity Liquid Nonionic 7.0 ± 1.0 1.15 ± 0.05 Easily soluble with all proportions in cold water. Min. 1 year under cool and dry conditions when stored in original sealed, packaging. Compatible with anionic, nonionic and cationic materials. - AC-K imparts effect of shortening time and water saving in washing process because it has good removal efficiency of peroxides. - AC-K prevents corrosiveness of equipment because it has rust-inhibitor effect. - AC-K removes even the peroxides inside organization of fibers because it has good penetrating efficiency. - It is environmental-friendly product as APEO-free and NPEO-free. AC-K is treated on the basis of 2~4 g/ℓ at 60~70℃ for 20~30min according to the treatment condition of peroxides bleaching and kind of fibers. 1. Removal treatment in Cold-Pad-Batch H2O2(35%) NaOH CAMINOL Room temp.∼40℃ X 10-20 hours |
| --- | --- |

| ◈ RECOMMENDED RECIPE | Washing hot (Boiling) |
| --- | --- |
|  | Washing hot (Boiling) |
|  | Removal treatment PO-K 2-4g/ℓ, Acetic acid 0.5cc/ℓ 60℃ X 20∼30 min. |
|  | Washing |
|  | 2. Removal treatment after Pad-Steam |
|  | H2O2(35%) NaOH CAMINOL Room temp.40℃ X 10-20 hours |
|  | 95-100℃ Steaming |
|  | Washing hot (Boiling) |
|  | Washing hot (Boiling) |
|  | Removal treatment PO-K 2∼4g/ℓ, Acetic acid 0.5cc/ℓ 60℃ X 20-30 min. |
|  | Washing |
| ◈ PACKAGE | 120 Kgs, 200 Kgs NET IN DRUMS. |