### QX-801 has strong penetrating ability and emulsifying/dispersing ability and can be applied to Polyester, Nylon, Cotton, Rayon and their blends. It is an alkali resistant scouring/emulsifying agent, which exhibits especially excellent efficiency even on Micro or thick high density fabric as well as general fabric.

◈ SPECIFICATION

#### APPEARANCE

- IONIC NATURE

- pH(As is)

- SP.GR(at 25℃)

- SOLUBILITY

- STORAGE STABILITY

- COMPATABILITY

◈ FEATURES

◈ APPLICATION FIBERS

◈ HOW TO USE

Yellowish Liquid Nonionic

7.5 ± 1.0

1.05 ± 0.05

Easily soluble in cold water.

Min. 1 year under cool and dry conditions when stored in original sealed, packaging.

Compatible with anionic and nonionic materials.

- QX-801 prevents a phenomenon of redeposition, because

QX-801 can penetrate deeply into fiber-cells by its strong penetrating ability and remove them by emulsifying/dispersing or solubilizing weaving oil and various stains.

- Because QX-801 has excellent alkali resistance, does not cause a phenomenon of gum up by alkali.

- QX-801 can be applied to the continuous scouring system, as well as

a regular scouring process, because it can show excellent scouring effect by its strong penetrating ability and alkali resistance.

- It is environmental-friendly product as APEO-free and NPEO-free.

Suitable for all fibers such as Polyester, Nylon, T/C, T/R, N/P, N/C, Acryl, Silk, etc.

Recommended use levels are 1∼4 g/ℓ according to kinds, density, thickness and types of fibers.

## ◈ RECOMMENDED RECIPE

#### Alkali scouring of Cotton and T/C goods

  - Winch or Jigger Scouring

    - 98% NaOH

#### QX-801

    - TS-CN

    - Scouring conditions

    - Washing conditions

    - Bath ratio

  - Kier-boiling Scouring

    - 98% NaOH

#### QX-801

    - TS-CN

    - Scouring conditions

    - Washing conditions

    - Bath ratio

  - Continuous Scouring

    - 98% NaOH

#### QX-801

    - TS-CN

    - Scouring conditions

: 6-10 g/ℓ

: 1-2 g/ℓ

: 0.5-1 g/ℓ

: Scouring for 60 min at 100℃.

: Washing hot and then cold.

: Winch (1:20), Jigger(1:4)

: 50 g/ℓ

: 1-2 g/ℓ

: 1 g/ℓ

: Scouring for 60 min at 100℃.

: Washing hot and then cold.

: 1:4

: 50-70 g/ℓ

: 2-4 g/ℓ

: 1 g/ℓ

: 30-50 m/min at 100℃

#### One bath scouring/bleaching of Cotton and T/C goods

  - Winch Scouring

    - 35% H2O2

    - 98% NaOH

#### QX-801

    - TS-CN

    - CAMINOLX

    - Scouring conditions

    - Washing conditions

    - Bath ratio

: 5-10 g/ℓ

: 2 g/ℓ

: 1-2 g/ℓ

: 0.5-1 g/ℓ

: 2-4 g/ℓ

: Scouring for 30∼60 min at 95-100℃

: Washing hot and then cold.

: 1:15-1:20

## ◈ RECOMMENDED RECIPE

  - Jigger Scouring

- 35% H2O2

- 98% NaOH

#### QX-801

- TS-CN

- CAMINOLX

- Scouring conditions

- Washing conditions

- Bath ratio

: 10-20 g/ℓ

: 2 g/ℓ

: 1-2 g/ℓ

: 0.5-1 g/ℓ

: 4-5 g/ℓ

: 4 Cycles at 95-100℃

: Washing hot and then cold.

: 1:4

  - Continuous Scouring

    - 35% H2O2

    - 98% NaOH

#### QX-801

    - TS-CN

    - CAMINOLX

    - Scouring conditions

    - Washing conditions

: 20-30 g/ℓ

: 3-4 g/ℓ

: 2-3 g/ℓ

: 1-2 g/ℓ

: 5-6g/ℓ

: 30-50 m/min at 95-100℃.

: Washing hot and then cold.

#### Continuous bleaching of desized cotton goods

- 98% NaOH

- 35% H2O2

#### CAMINOLX

- QX-801

- Scouring conditions

- Washing conditions

: 10-15 g/ℓ

: 30-50 g/ℓ

: 6-10g/ℓ

: 1-3 g/ℓ

: Steaming for 5-20 min.

: Washing hot and then cold.

## ◈ RECOMMENDED RECIPE

#### C.P.B recipe for 100% cotton goods

- 98% NaOH

- 35% H2O2

#### CAMINOLX

- QX-801

- TS-CN

- Pick Up

- Padding temperature

- Batching time

: 35 g/ℓ

: 60-80 g/ℓ

: 8-12g/ℓ

: 8-12 g/ℓ

: 1-2 g/ℓ

: 90%

: 25℃

: 18-24 hours

#### The method to remove finishing oils

- Na2CO3

#### QX-801

- Scouring conditions

- Washing conditions

: 2-3 g/ℓ

: 2-3 g/ℓ

: Scouring for 30-60 min at 80-95℃

: Washing hot and then cold.

◈ PACKAGE

120 Kgs NET IN DRUMS.